## Slide 1: Feedhorn antennas for upGREAT
high performance feedhorns
  smooth-walled spline profile (Granet 2004, Zeng 2010)
  optimized beam characteristics in 3D-EM modeller and fabricated by electroforming (Radiometer Physics GmbH)
  1.9 – 2.5 THz (wideband), 4.7 THz
  specs FPBW(-10 dB)=19.5°, G=25 dBi
M1.6
0.7 mm aperture
4.7 THz feedhorn
2.4 mm
circ. to rect.
WG transition

## Slide 2: Feedhorn-mixer interface
xxx
4 mm

## Slide 3: Fabrication of waveguide devices
NbN deposition @ 1000°C

## Slide 4: Fabrication of waveguide devices
few nm thin superconducting microbridge layer is crucial for HEB performance characteristics
  e.g. IF bandwidth, LO power consumption
  NbN now replaces NbTiN as superconductor (higher IF)
2 µm thin membrane substrates
  Si now replaces SiN (higher IF)
  SOI wafer used for processing
  DRIE definition for substrate shaping
fabrication split into frontside and backside processing
  DC IV characterisation in-between
all fabrication incl. NbN layer in-house

## Slide 6: Device fabrication frontside

## Slide 7: Device ready for IV tests

## Slide 8: SOI wafer
348 HEB plus test devices
IV characterization before backside processing
backside processing on individual sections
30 mm
after frontside processing
diced for IV characterization

## Slide 9: DC device characterization
18 devices after front side processing
80 Ohm
120 Ohm
35 of 36 devices
after front side processes
120 Ohm
80 Ohm
device uniformity across wafer crucial for equal LO power consumption in array receiver
RT
IV

## Slide 10: Device fabrication backside

## Slide 11: Fishing for devices …

## Slide 12: 4.7 THz waveguide HEB device
1250 µm
IF output and DC connection
RF input section

## Slide 13: 4.7 THz waveguide HEB device
RF part with waveguide, probe antenna, transmission line chokes and HEB microbridge
beamlead

## Slide 14: RF section of 4.7 THz HEB device
waveguide
probe antenna
microstrip transmission line
with impedance matching
and choke sections
HEB
microbridge
alignment
window
l/4 high Z
line to ground
2 µm Si
membrane
substrate
3 µm electroplated
Au beamlead
waveguide
window

## Slide 15: HEB microbridge with contacts
5 nm x 300 nm x 3600 nm x 5 nm NbN microbridge

## Slide 16: Device mounted and contacted
750 µm
HFA device